## Slide 1
OMICS International welcomes submissions that are original and technically so as to serve both the developing world and developed countries in the best possible way.
OMICS Journals are poised in excellence by publishing high quality research. OMICS International follows an Editorial Manager® System peer review process and boasts of a strong and active editorial board.
Editors and reviewers are experts in their field and provide anonymous, unbiased and detailed reviews of all submissions.
The journal gives the options of multiple language translations for all the articles and all archived articles are available in HTML, XML, PDF and audio formats. Also, all the published articles are archived in repositories and indexing services like DOAJ, CAS, Google Scholar, Scientific Commons, Index Copernicus, EBSCO, HINARI and GALE.
For more details please visit our website: http://omicsonline.org/Submitmanuscript.php
OMICS Journals are welcoming Submissions

## Slide 2
P. S. Wei
Xi-Wan Chair Professor
Department of Mechanical and Electro-Mechanical Engineering
National Sun Yat-Sen University
Kaohsiung, Taiwan 80424, ROC
E-mail: pswei@mail.nsysu.edu.tw
Heat Transfer Lab for Manufacturing and Materials Processing
NSYSU
Mechanical & Micro-Mechanical Engineering
Understanding of workpiece defects induced by laser beam
Journal of Lasers, Optics and Photonics

## Slide 3
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
This presentation deals with (1) defects of surface rippling and humping and root spiking and (2) pore formation due to super-saturation and liquid entrapment after solidification. Surface rippling and humping often accompany solute segregation, porosity, crack, deformation, etc. Spiking accompanies cold shut and porosity is another severe defect. Incapable drilling also results from collapse of the induced keyhole. Finding mechanisms of these defects is essentially required to control qualities of workpieces.
Abstract

## Slide 4
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Introduction
Laser welding or melting (http://www.rofin.com/en/applications/laser_welding/welding_methods/)

## Slide 5
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
TORVAC EBW, max. 60 kV, 50 mA, 60 mm/s, 3000 W
Experimental setup

## Slide 6
Rippling and spiking are decreased by increasing welding speed. Porosity can also be seen near the spiking tip (Wei et al. 2012, IEEE Trans. CPMT)
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Observation and measurements

## Slide 7
Spiking and humping are decreased by increasing welding speed and raising focal location. Porosity can also be seen near the spiking tip (Wei et al. 2012. IEEE Trans. CPMT)
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
(continued)

## Slide 8
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
(continued)
Spiking tendency by considering energy conservation in welding and
vertical directions is given by (Wei et al. 2012, IEEE Trans. CPMT)
where melting efficiency is

## Slide 9
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
(continued)
Average pitch of humping or spiking for alloys in the absence and presence of volatile elements are, respectively,

## Slide 10: Pore formation
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Bubble nucleated due to super-saturation
Pore formation due to liquid entrapment in keyhole welding
(Pastor et al. 2001, Weld. Int.)

## Slide 11
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Experimental setup
Experimental Setup (Wei et al. 2003, Metall. Mater. Trans B;
Wei et al. 2004, JCG)

## Slide 12: Bubbles trapped in solid at different times or locations near the location of 1 cm (a) 0, (b) 5, (c) 20, (d) 60, (e) 120, (f) 150, (g) 180, and (h) 206 s during the freezing of water containing oxygen gas content of 0.0041 g/100 g and temperature of the constant temperature sink of -250C (Wei et al. 2004, JCG).
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
(continued)

## Slide 13: Bubbles trapped in solid at different times or locations near a location of 1 cm (a) 0 s,(b) 450 s, (c) 540 s, (d) 810 s, (e) 900 s, (f) 1170 s, (9) 1350 s, (h) 1440 s during the freezing of water containing oxygen gas content of 0.0037 g/100 g and temperature of -250C of the constant temperature sink (Wei et al. 2004).
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
(continued)

## Slide 14
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Pore formation due to super-saturation
Differentiating equation of state with time
Mass transfer to the bubble is given by
Henry’s law is
Volume change rate is

## Slide 15: (continued)
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Development of pore shape for dR/ds= 0.04sin(0.4s) (Wei and Hsiao, 2012)

## Slide 16: (continued)
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Equations of mass, momentum are, respectively

## Slide 17: (continued)
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Conservation equations of energy, concentration and phase field equations are, respectively

## Slide 18
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
(continued)
Predict pore formation in aluminum

## Slide 19: Pore formation due to liquid entrapment
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Equations of mass, momentum and energy are, respectively
The higher the gas pressure, the easier and smaller the pore can be formed

## Slide 20: (continued)
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Pore formation or keyhole collapse for energy absorption for a supersonic flow (Wei et al. 2014, IEEE Trans. CPMT)

## Slide 21: Conclusions
NSYSU
Mechanical & Micro-Mechanical Engineering
Heat Transfer Lab for Manufacturing and Materials Processing
Mechanisms of different types of surface patterns such as rippling, gouging, undercut, and humping, and root spiking are still unclear.
Pore formation is characterized by different mechanisms: (1) super-saturation of dissolved gases in liquid ahead of the solidification front, and (2) liquid entrapment such as keyhole collapse during keyhole welding.
All these defects involve strong deformation of the free surface and different types of instabilities coupled with complicated transport processes. Controlling factors need to be clarified and determined.

## Slide 22: Journal of Laser Optics & Photonics
Journal of Photonics
Journal of Wave theory
Journal of Optics
Journal of Lasers
Signal Crystal

## Slide 23: Journal of Laser Optics & Photonics
For upcoming Conference visit
http://www.conferenceseries.com/